|  | ZHENGZHOU STEELL METAL CO.,LTD |
| --- | --- |
|  | Tel:0086 371 86080791 Fax:0086 371 67221140 E-mail:steellmetal@126.com |

FERRO ALLOY PRODUCTS DATASHEET

- FERRO SILICON – Inoculant

| FESI68 | Chemical composition% |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si |  | Ca max | Ba max |  |  | Al max | Moisture max | P max | S max |
|  | 68-70 |  | 1.5 | 1.0 |  |  | 1.5 | 0.05 | 0.05 | 0.05 |
| Bulk density |  | approx 2.7g/cm3 |  |  | 1000Kg bags or on pallet approx 24MT/20FCL |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:200MT/month; |  |  |  |  |  | Conventional grain size:0.1-0.4mm 90%min |  |  |  |  |

- RARE EARTH FERRO SILICON MAGNESIUM – Nodulizer

| REFESIMG 3-8 | Chemical composition% |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si |  | Ca | Mg |  |  | Re | Al max | P max | S max |
|  | 44-45 |  | 1-2 | 3-8 |  |  | 1-3 | 0.6 | 0.05 | 0.05 |
| Bulk density |  | approx 2.9g/cm3 |  |  | 1000Kg bags or on pallet approx 25MT/20FCL |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:180MT/month; |  |  |  |  |  | Conventional grain size:1-3mm,3-15mm,5-25mm |  |  |  |  |

- CALCIUM SILICON ALLOY –Deoxidant

| CASI 28-30 | Chemical composition% |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Si |  | Ca min | C max |  |  | Ba max | Al max | P max | S max |
| Ca30Si60 | 60-65 |  | 30 | 2.0 |  |  | 0.5 | 1.5 | 0.06 | 0.05 |
| Ca28Si55 | 55-60 |  | 28 | 2.0 |  |  | 0.5 | 1.5 | 0.06 | 0.05 |
| Bulk density |  | approx 2.3g/cm3 |  |  | 1000Kg bags or on pallet approx 22MT/20FCL |  |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |  |
| Supply quantity:200MT/month; |  |  |  |  |  | Conventional grain size:0-3mm,10-100mm,50-100mm |  |  |  |  |

- ALUMINUM – Deoxidant for LAF, LADLE

| Al-20 | Chemical composition% |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | M-Al |  | Al2O3 | SiO2 max |  |  | Moisture max | P max | S max |
|  | 15-30 |  | 30-60 | 15 |  |  | 1.0 | 0.05 | 0.05 |
| Bulk density |  | approx 1.9g/cm3 |  |  | 1000Kg bags or on pallet approx 20MT/20FCL |  |  |  |  |
| Packing : 1000Kg bags, 25Kg paper bags , 1000Kg on pallet, or as users detail requirements. |  |  |  |  |  |  |  |  |  |
| Supply quantity:300MT/month; |  |  |  |  |  | grain size: 10-60mm Briquettes; 0.5-5mm |  |  |  |

Regarding our company contents and other products ,please glance over:

www.steellmetal.com  ,  www.resteellmetal.com